## Slide 1
Alkali Soluble Rheology Modifier
www.reachinchem.com

## Slide 2
Benefits
Effective suspension of insoluble, difficult to suspend components or particles, such as anti-dandruff agent, silicone oil, petal, bead, etc
Has excellent transparency in transparent formula and enhances pearlescent effect in pearlescent products
Liquid, easy to use, with stabilizing, thickening and co-emulsifying functions
Has excellent salt resistance and good compatibility with anionic and nonionic surfactants
A special rheology modifier for transparent or suspension formulas-Repoly 100

## Slide 3
Formulation process appearance
Step 1
Water
Repoly 100：7%
pH = 3.0
Step 2
Water
Repoly 100：7%
SLES：18%
CDEA ：2%
pH = 5.5
+ 32%NaoH
+ 32%NaoH
pH = 6.5
pH = 6.9

## Slide 4
A special rheology modifier for transparent or suspension formulas-Repoly 100
Specification
Item | Specification
Appearance(25℃) | Milky white liquid
Solid content(%) | 34.0-36.0
pH | 2.1-3.8
1%solids aqueous solution(mPa·s) | 4000-8000
Residual ethyl acrylate(mg/kg) | 0-1.0

## Slide 5
Thickening mechanism
Activated polymer
H2O
H2O
H2O
H2O
H2O
H2O
H2O
H2O
OH-
Alkali
Swellable
Emulsion Thickeners
Unactivated Polymer

## Slide 6
Effect of active content on the viscosity and transmittance of water solution
Performance comparison
The viscosity of neutralized water solution increases with the increasing of active content, Repoly 100 is better than Polymer C on viscosity. For the transmittance, Repoly 100 shows an increasing trend with the increasing of active content, while polymer C shows a decreasing trend after a small increasement, the transmittance of Repoly 100 is better than Polymer C.
(We compare with polymer C from competitor)

## Slide 7
Effect of pH value on the viscosity and transmittance of water solution
Performance comparison
The viscosity of neutralized water solution is stable within the range of pH=7.0 to pH=11.0, and Repoly 100 exhibits a better thickening efficiency compared with Polymer C. The transmittance isn’t affected by the pH value within the given range, except for the transmittance of 2% Polymer C’s solution decreases with the increasing of pH value.
(We compare with polymer C from competitor)

## Slide 8
Electrolyte resistance of Repoly 100
Performance comparison
The electrolyte resistance of Repoly 100 is very good, especially for the large polymer amount solution.
(We compare with polymer C from competitor)

## Slide 9
INCI Name | Weight % | Function
Deionized Water | To 100 | Diluent
SLES, 2EO, 70% | 16 | Surfactant
Acrylates Copolymer, base on solid | 2.1 | Rheology Modifier
Sodium Hydroxide, 18% | Base on the pH control | Neutralizer
Cocamidopropyl Betaine, 35% | 14.3 | Surfactant
Kathon, 2.5% | 0.06 | Preservative
Effect of pH value on performance of a typical formula
Performance comparison

## Slide 10
Effect of pH value on performance of a typical formula
Performance comparison
The yield value of Repoly 100 is larger than polymer C in this test formula, especially with the low pH value.
(We compare with polymer C from competitor)

## Slide 11
Effect of electrolyte on performance of a typical formula
INCI Name | Weight % | Function
Deionized Water | To 100 | Diluent
SLES, 2EO, 70% | 16 | Surfactant
Acrylates Copolymer, base on solid | 2.1 | Rheology Modifier
Sodium Hydroxide, 18% | Adjust pH=6.8 | Neutralizer
Cocamidopropyl Betaine, 35% | 14.3 | Surfactant
Sodium Chloride | 0, 0.2, 0.4, 0.6, 0.8 | Electrolyte
Kathon, 2.5% | 0.06 | Preservative
Performance comparison

## Slide 12
Effect of electrolyte on performance of typical formula
Performance comparison
The yield value of Repoly 100 is larger than polymer C in this test formula. When the electrolyte content is more than 0.4%, the transparency shows a decreasing trend, and the performance is basically the same.
(We compare with polymer C from competitor)

## Slide 13
INCI Name | Weight % | Function
Deionized Water | To 100 | Diluent
SLES, 2EO, 70% | 16 | Surfactant
Acrylates Copolymer, base on solid | 2.1 | Rheology Modifier
Sodium Hydroxide, 18% | Adjust pH=6.8 | Neutralizer
Cocamidopropyl Betaine, 35% | 20, 14.3, 8.57, 2.86 | Surfactant
Kathon, 2.5% | 0.06 | Preservative
Effect of CAB on the performance of a typical formula
Performance comparison

## Slide 14
Effect of CAB on the performance of a typical formula
Performance comparison
With the increase of CAB content, the viscosity of tested formula showed an upward trend. When the content of CAB was more than 15%, the viscosity of Repoly 100 is larger than polymer C. The addition of CAB had no significant effect on the transparency of the formula.
(We compare with polymer C from competitor)

## Slide 15
Effect of SLES-2EO on performance of a typical formula
INCI Name | Weight % | Function
Deionized Water | To 100 | Diluent
SLES, 2EO, 70% | 8, 12, 16, 20 | Surfactant
Acrylates Copolymer, base on solid | 2.1 | Rheology Modifier
Sodium Hydroxide, 18% | Adjust pH=6.8 | Neutralizer
Cocamidopropyl Betaine, 35% | 14.3 | Surfactant
Kathon, 2.5% | 0.06 | Preservative
Performance comparison

## Slide 16
Effect of SLES-2EO on performance of a typical formula
Performance comparison
With the increase of SLES-2EO content, the viscosity of tested formula showed an upward trend, and the viscosity of Repoly 100 is larger than polymer C. When the content of SLES-2EO is more than 12%, Repoly 100 shows better transparency.
(We compare with polymer C from competitor)

## Slide 17
Ingredients | % w/w
Aqua | TO100
SLES (70%) | 16
Repoly100 | 7
NaOH | q.s
DOE120 | q.s adjust viscosity
CAB 35 | q.s adjust viscosity
Preservative | 0.06
Test formula
Formula finished
status
Keep at 48℃
for 1 week
Repoly 100 7% Repoly100 7% Polymer C
Viscosity 20000cps Viscosity 30000cps Viscosity 30000cps
Suspending performance
(We compare with polymer C from competitor)

## Slide 18
Ingredients | % w/w
Aqua | TO100
SLES (70%) | 16
Repoly100 | 7
NaOH | q.s
DOE120 | q.s adjust viscosity
CAB 35 | q.s adjust viscosity
Preservative | 0.06
Test formula
Keep at 48℃ for 4 weeks
Repoly 100 7% Repoly100 7% Polymer C
Viscosity 20000cps Viscosity 30000cps Viscosity 30000cps
✎ test result: suspending effect related to dosage of Repoly 100, but not to viscosity of formula.
Suspending performance
(We compare with polymer C from competitor)

## Slide 19
Synergy with Sodium Chloride
Formula | %
Water | To100
Repoly 100 | 5.0
SLES (30%) | 39
32%NaOH | to pH 6.7-7.0
CAPB (30%) | 8.0
NaCl | 0，0.5，1，1.5
Chart: NaCl dosage
| 0 | 0.005 | 0.01 | 0.015
 | 1220 | 1920 | 4360 | 8700
Sodium Chloride has the feature to thicken efficiently surfactants based formulation at concentration tipically ; the synergy between Sodium Chloride and Repoly 100 permits to reach high viscosity

## Slide 20
Effect on the foam
In the figure below we show the effect of different % of Repoly 100 on the foaming action of a basic bubble bath formula compared to a classical surfactant systemviscosifier.
Formula | %
Water | To100
Repoly 100 | 0，5，7，9
SLES (30%) | 39
32%NaOH | to pH 7.0
CAPB (30%) | 8.0
Ross Miles Foam test in water
Chart: Repoly 100 dosage
| 0 | 0.05 | 0.07 | 0.09
0min | 140 | 140 | 140 | 140
5min | 140 | 140 | 140 | 140
The addition of Repoly 100 has not a significant effect on the foam behaviour of the finished formulation.

## Slide 21
Shower gel
Formula with ethanol, isopropanol, propylene glycol and glycerol
Shampoo
Foundation
Sunscreen
Facial Cleanser
Application
Acrylates Copolymer has been used as many as 70070 times in all commodities. The data comes from Meilixiuxing app.

## Slide 22
The recommended dosage is 5-8% in the surfactant system and more than 7% of the suspended particles
In order to achieve the best effect, the total amount of surfactant is recommended to be added to 15-23%
In order to achieve the best transparency, it is suggested to adjust the pH to 6.5-7.0
The recommended dosage is 3-5% in emulsion system
Repoly 100
Formula Guidelines

## Slide 23
Product on marketing
DOVE Botanic Selection Shampoo
Acrylates Copolymer, as a suspension stabilizer, can effectively suspend petals

## Slide 24
Product on marketing
Ryo Deep Cleansing Scalp Care Shampoo
Acrylates Copolymer, as a suspension stabilizer, can effectively suspend beads and anti-dandruff agent

## Slide 25
Product on marketing
SK-II Atmosphere Airy Light UV Cream
Acrylates Copolymer can stabilize the system and form water resistance film on skin

## Slide 26
Product on marketing
Elta MD foaming facial cleanser
Acrylates Copolymer can stabilize the system and make foam easy to rinse, no residue

## Slide 27
Product on marketing
Maybelline FIT me foundation
Acrylates Copolymer can stabilize the system and form water resistance film on skin

## Slide 28
Reference formula
Clear bath gel with beads
Chocolate Scrub Shower Gel
Clear bath gel with ice crystal

## Slide 29
Reference formula
Pearly bath gel
Quicksand shower gel

## Slide 30
Reference formula
Effectively suspend silicone oil emulsion and opacifier, stabilize formulation system
Effectively stabilize formulation system, and solve the problem of soap base instability and easy coarsening
Effectively thicken and stabilize formulation system

## Slide 31
If you are interested in these products, please contact us!
Thank you!
【Telephone】
020-37087379
【E-mail】
helena@reachinchem.com